Supporting:  LMFFL2004A Moisture test timber and concrete floors
LMFFL3101A Inspect sub-floors

# Section 3 Assignment: Measuring moisture and pH

| Name |  | Date |  |
| --- | --- | --- | --- |

Provide short answers to the following questions:

- How do capacitance moisture meters work, and why are they not very accurate for taking moisture readings in concrete floors?

- Capacitance moisture meters are still useful devices to have on hand when you’re testing a concrete floor. What are they good for?

- When you carry out a ‘surface mounted hood test’, exactly what are you measuring? What is the maximum RH permitted in a concrete slab when tested in this way?

- When you carry out an ‘in-situ probe test’, exactly what are you measuring? What is the maximum RH permitted in a concrete slab when tested in this way?

- How does an electrical resistance moisture meter measure the amount of water that’s present in timber? What is the normal allowable moisture content range for timber in a subfloor?

- Why is the ‘calcium chloride test’ no longer used by flooring installers to measure moisture content in concrete?

- How many moisture tests should be carried out on a 100 m2 floor?

- List the types of details you should record when you carry out a set of moisture tests on a subfloor (as recommended by the Australian Standards).

- Why is it important to know what the pH level is on the concrete surface before you start a vinyl flooring installation?